| Procedure for the fabrication of dumbbell and DMTA specimens for quality assurance testing |  |
| --- | --- |
| Specimens required: 5 Dumbbells and 3 DMTA strips (unless otherwise stated) |
| Equipment required: (Ensure all equipment is ready before work commences) Mould for casting specimens (Fig.1) Release agent Spatula / small trowel |
| Procedure: Ensure all equipment is clean and free from contamination Open mould and coat all surfaces that will have contact with the adhesive with release agent (WARNING – Take care to not spray release agent near to anything to be bonded – e.g. away from site and down wind) Mix the adhesive as recommended by the adhesive supplier (DO NOT add any ballotini or bondline spacers to the adhesive) Apply the adhesive liberally over the mould ensuring that each cavity has been slightly over-filled. Take care to avoid air pockets as these will cause voids in the specimens, rendering them unsuitable for testing Close the mould and tighten the bolts starting from the centre. Progressively tighten bolts, as shown in the Fig.2, to ensure the mould plates are kept parallel Fig.1 Dumb bell and DMTA mould and specimens Fig.2 Bolt-tightening sequence Remove excess adhesive from edges of joint with a spatula. Place mould next to the actual job and allow adhesive to cure on-site Record date, time, temperature, humidity and adhesive batch numbers on the corresponding specimen information sheet. |
| TIPS: Spray release agent on bolts and in threads to aid in mould disassembly Retighten bolts after 2 minutes, as they will loosen as excess adhesive is extruded from the mould. |
| Note: | This sheet is for guidance only. Please also refer to adhesive manufacturer’s data and safety sheets. |

# Text boxes

3rd

1st

4th

2nd

6th

7th

5th

8th